RENSON LOUVRE SPECIFICATIONS

Brand		: LOUVRE PANEL

Type 		: 431WK2 – BURGLAR-PROOF 33mm pitch wall louvre

Manufacture and reference :

The 431WK2 Louvre Panel is manufactured and supplied by Renson Fabrication Ltd.  Tel: 01622 754123

Email: louvres@rensonuk.net Website: www.renson.eu

Description:

RENSON 431WK2 is an extruded aluminium louvre panel using a burglar proof blade mounted into an integrated frame. It is designed to be built into a pre formed opening. It is supplied without a flanged frame.

System operation and Airflow Performance:

Type				431WK2

Visual Free Area		59%

Physical Free Area		41%

K-factor: Intake			23.6

K-factor: Discharge		25.5

Ce coefficient: Intake		0.206

Cd coefficient: Discharge	0.198

Burglarproof

Louvre 431WK2 is burglarproof according to class RC2, certificate surface 0,306 < o < 1,875 m², in accordance with EN1627 up to and including EN1630 (September 2011).

Dimensions/Size Range:

Minimum Dimensions (mm)	200 x 200

Thickness (mm)		31

Pitch (mm)			33.3

Product Construction:

Profile: Extruded aluminium (EN 12020-2)

Surface Treatment:

Mill finish

Anodised (EV6/EV1) (20 micron): pre-treated and anodised.

Polyester powder coating in any RAL colour (40 micron): aluminium profiles pre-treated to resist corrosion to guarantee.

Installation:

Surface mounted louvre. The louvre must be mounted using burglar resistant screws. Burglar resistant screws type Secufast® Pin Hexagon Ø 4.2 x 38 mm.

Reinforcing structure required for panels larger than 3m2.

Accessories

Stainless steel birdguard 6mm x 6mm secured to the rear

Stainless steel insect mesh 2.3mm x 2.3mm secured to the rear

Backframe, pre-installation frame, water channel, drainage channel

Product Information:

http://www.rensonuk.net/Louvres-panels-United-Kingdom.html